## Slide 1
Development of Stitched Composites for Advanced Aircraft Part II: Pressure Cube and Hybrid Wing Body Center Section Test Article
NESC Academy Webcast
Moderated by Dr. Ivatury Raju
NASA Technical Fellow for Structures
NASA Engineering & Safety Center (NESC)
Adam Przekop, Dawn Jegley NASA Langley Research Center

## Slide 2: Participants
NASA Langley Research Center
Boeing Research and Technology

## Slide 3: Objective of Presentations
  Part I, presented on October 5, 2016 by Dawn Jegley, described the structural concept, background, and the building blocks in development of the concept
  Part II describes the design, analysis, and testing of the pressure cube and the large-scale hybrid wing body (HWB) center section test article

## Slide 4: Outline
Questions from Part I
Background
Building blocks
  Individual stiffeners
  Individual panels
  Build up structure (pressure cube)
HWB center section test article
Discussed in Part I
(TRL 3-4)
Subject of Part II
(TRL 5)

## Slide 5: Questions from Part I
How is stitching with PRSEUS different from stitching from the Advanced Composites Technology program?
Could you compare and contrast the PRSEUS stitching vs Z-pinning that is currently used?
What would the differences be for wing structures compared to what is used on multi-bay box?
The objective is a structural weight savings of ten percent. How does this translate to airplane weight?
Stitching
Frame
Stitching
Stitching
Precured Rods
Stitching
Skin
Stringer
PRSEUS = Pultruded Rod Stitched Efficient Unitized Structure

## Slide 6: HWB Airframe Development
Test
Loads
Coupons/Elements
Trade Studies
Panel Geometry
Result
PRSEUS 10.4% lighter.
…improved buckling performance.
Combined axial & pressure loading
Weight Goals
…10% better than sandwich.
…withstand 2P
(18.4 psi) load case.
…arrested damage at 1.5 times initiation load.
…within 5% of static results after 2 fatigue lives.
…global panel buckling at -75 kips per frame.
Compression
Panel
Trades
Rod-Stiffener
Frame
Tension Panel
Pressure Panel
Pressure
Cube
HWB Center Section Test Article

## Slide 7: Building Block Testing
Trades Studies
Panel Geometry
Weight Goals
Test
Loads
Stability
Tension Loading
Damage
Arrestment
Repair
Flexure Coupons
Pressure Panel
Pressure Cube
Pressure Loading
Stringer
Stability
Post-Buckled Structures
Strength
Compression Loading
Biaxial Loading
Adhesion
Frame Stability
Fail-Safe
Pressure and Bending
Test in Combined Loads Test System (COLTS) Facility
HWB Center Section Test Article

## Slide 8: HWB Configuration of Interest
HWB Center Section
Structural challenge: performance and manufacturability of the pressurized non-circular center section
Design Characteristics
• Wing Area (trap) = 4,003 ft2
• Wing Span = 185.7 ft
• Wing Sweep = 35.5º
• Cruise = .85 Mach
• Range = 7,500 nm
• MTOW = 408,700 lbs
• MLW = 289,100 lbs
• MZFW = 273,100 lbs
• Payload = 44,310 lbs
HWB Center Section

## Slide 9: HWB Vehicle Center Section Loads
Span-wise
Stream-wise
Pressure

## Slide 10: Pressure Cube Test Objectives
Design and verify integral joint concept
Pressurized Cube Design
52-in. by 48-in. by 56-in.
Large-Scale Test Article
Pressure cube loads
scaled up to match HWB center section joint loads

## Slide 11: Pultruded Rod Stitched Efficient Unitized Structure (PRSEUS) Concept
Highly integrated and light-weight (fewer joints)
Damage tolerant (delamination- and crack-arresting capabilities)
Cost effective (made of stitched dry fabric preforms, resin infused, no metal inner moldline tools and no autoclave required)
Stitching
Foam Core
Frame Stacks
Stringer Tear Strap
Stitching
Stitching
Precured
Rods
Keyhole for Stringer Pass-thru
Stitching
Frame Cap
Stacks
Skin Stacks
Stringer
Stacks
Stringer CL
Test Article:
Stringers:
1.65-in. tall, 6-in. spacing
Frames:
6.00-in. tall, 24-in. spacing
1 Stack  0.052 in. 7 Plies (+45, -45, 0, 90, 0, -45, +45) (0º  44.9%, ±45º  42.9%, 90º  12.2%)

## Slide 12: Typical PRSEUS Panel Substructure Spacing
Stringer with Pultruded Rod
Sandwich Frame
Rod
Web
Flange
Skin
Flange
Foam
Facesheet
6 in.
24 in.
1.65 in.

## Slide 13: Integral T-Cap Joint Concept
Reduced complexity by using T-Caps integrally built into panels
Reduce number of aluminum fittings required along panel edges

## Slide 14: Pressure Cube Manufacturing
First PRSEUS panels successfully built with integral T-cap joints

## Slide 15: Pressure Cube Test Instrumentation
11 Displacement transducers
168 strain gauges
Video Image Correlation in 3D (VIC-3D) on two side panels
Exterior and interior cameras
Non-destructive evaluation (NDE)

## Slide 16: Pressure Cube Test Loads and Conditions
Pristine tests
  NDE as manufactured
  Check-outs up to 0.5P
  Preliminary test to 1.0P
  Final pristine test to 2.2P
  NDE after pristine tests
Barely visible impact damage (BVID) tests
  100 ft-lbs external BVID applied
  Additional NDE performed in the vicinity of BVID application
  Pressurized to failure
  P = 9.2 psi

## Slide 17: Pressure Cube Model and Analysis
Finite Element Analysis (FEA) using MSC.NASTRAN
  Global linear and nonlinear
  Local joint analysis with contact interactions and nonlinear material properties
253,575 nodes 279,056 elements 2,144 fastener connections

## Slide 18: Pressure Cube Predictive Analysis
Global nonlinear FEA
  Sample displacement results
Deformation under 28.5 psi

## Slide 19: Pressure Cube Predictive Analysis, cont’d
Global nonlinear FEA
  Pressure cube to HWB center section bending moment scaling at the ends of bulkhead frames
Factor = 390/166 = 2.35
 Cube must demonstrate 2.35 x 18.4 psi (2P) = 43 psi (4.7P) for equivalent bending moment
Pressure Cube
HWB Center Section

## Slide 20: Pressure Cube Predictive Analysis, cont’d
Local FEA
  Integral T-caps
  Metallic fittings
Delamination in T-Cap at ~12.4 psi
(above the limit load, to be arrested by stitching)
Metallic fitting failure at ~47 psi

## Slide 21: Pressure Cube Test to Failure

## Slide 22: Pressure Cube Test to Failure

## Slide 23: Pressure Cube After Failure at 48 psi

## Slide 24: Initial Local Failure – Pristine Test
Local displacement and strain “jumps” at 16 and 19 psi
  No visible damage up to 20 psi (2.2P)
Displacement, in.
0.00 0.01
25
20
15
10
5
0
Pressure, psi
Strain, µε
0 500
Pressure, psi
25
20
15
10
5
0
Crown Panel Surface above T-Cap
Crown Panel Skin near T-Cap (Inside and Outside)
Crown
Panel
Crown
Panel

## Slide 25: Initial Local Failure – Pristine Test, cont’d
Delaminations, arrested at stitch lines, found during post-pristine test NDE (ultrasound)
Regions of delamination

## Slide 26: Location of the Final Failure Origination
Crown

## Slide 27: Final Failure Origination in Metallic Fitting

## Slide 28: Pressure Cube – Conclusions
Assembled PRSEUS panels exceeded the 18.4 psi (2P) overpressure loading requirement
Cube failed at 48 psi (5.2P)
  Integral T-cap joint design successfully sustained the 43 psi (4.7P) scaled-up load requirement equivalent to the HWB center section loading
  Metallic fitting likely originated the final failure sequence
Local damage arrestment above limit load successful due to stitching of integral T-caps

## Slide 29: HWB Center Section Test Article Schematic
Center Keel Panel
Floor Panel
Upper Inner Rib Panel
Crown Panel
Aft Lower Bulkhead Panel
Outer Rib Panel
Side Keel Panel
Lower Inner Rib Panel
Aft Upper Bulkhead Panel
Lower
Adaptor
Upper
Adaptor
30-foot long
14-foot
tall
7-foot
deep
Note: Fwd Bulkhead Panels
Removed for Clarity
11 PRSEUS panels and 4 composite sandwich panels

## Slide 30: HWB Center Section Test Article As Built

## Slide 31: Loads and Boundary Conditions
Maneuvering loads: wing up- and down-bending (2.5-g and −1-g)
Maneuvering loads with internal pressure (P = 9.2 psi): 2.5-g + 1P and −1-g + 1P
Over-pressure: 2P
Boundary Conditions (Uz=0)
Boundary Conditions (Uy=0)
Boundary Conditions (Uy,Uz=0)
HWB Center Section
Boundary Conditions (Ux,Uy,Uz=0)
(Rx,Rz=0)
Load
2.5-g Applied
Load
2.5-g Applied

## Slide 32: Load Cases
Summary of load cases
Beyond DUL load sequence
DLL – Design Limit Load
DUL – Design Ultimate Load
Load Case | DLL | DUL | Beyond DUL
Wing Down-Bending | -1.0-g | -1.5-g | N/A
Wing Down Bending with Pressure | -1.0-g + 1P | -1.5-g + 1.5P | N/A
Pressure-Only | 1.33P | 2P | N/A
Wing Up-Bending | 2.5-g | 3.75-g | 4.125-g
Wing Up-Bending with Pressure | 2.5-g + 1P | 3.75-g + 1.5P | 4.125-g + 1.5P

## Slide 33: Combined Loads Test System (COLTS)
HWB Center Section
Platen
Platen
Hydraulic Actuators

## Slide 34: HWB Test Article Installed in COLTS

## Slide 35: Finite Element Model
Element types used in the finite element model (FEM)
  1-D (bar) elements used for pultruded rods and frame tops
  2-D (shell) elements used for composite panels and metallic fittings
  Fastener (connector) elements used for bolted joints
Typical element size approximately 1 in.
Total model size approximately 4.5-million degrees of freedom
FEM Summary:
746,000 Nodes
745,000 Beam and Shell Elements
19,000 Connector Elements

## Slide 36: Instrumentation
Results to be discussed based on
  VIC-3D full field displacement acquisition on outer moldline (OML) surfaces of crown and upper bulkhead panels
  Strain gauges (362 unidirectional and 36 rectangular rosettes, total 470 channels)

## Slide 37: 2P: Upper Bulkhead Panel
Out-of-plane deformation at DUL

## Slide 38: 2P: Upper Bulkhead Minimum Gauge Skin
Back-to-back strains up to DUL

## Slide 39: 2.5-g: Crown Panel
Out-of-plane deformation at DUL
Frame
Frame
Frame
Frame

## Slide 40: 2.5-g: Crown Panel Out-of-Plane Deformation

## Slide 41: 2.5-g: Crown Panel Out-of-Plane Deformation

## Slide 42: 2.5-g: Center Frame of Crown Panel
Strains up to 165% DLL

## Slide 43: 2.5-g: Crown Panel Skin
Minimum principal strains up to 165% DLL

## Slide 44: 2.5-g: Crown Panel Minimum Gauge Skin
Back-to-back strains up to 165% DLL

## Slide 45: 2.5-g: Upper Bulkhead Panel
Out-of-plane deformation at DUL

## Slide 46: 2.5-g: Upper Bulkhead Out-of-Plane Deformation

## Slide 47: 2.5-g: Upper Bulkhead Out-of-Plane Deformation

## Slide 48: 2.5-g: Upper Bulkhead Minimum Gauge Skin
Principal strains up to 165% DLL

## Slide 49: 2.5-g + 1P: Crown Panel
Out-of-plane deformation at DUL
Frame
Frame
Frame
Frame

## Slide 50: 2.5-g + 1P: Crown Panel Out-of-Plane Deformation

## Slide 51: 2.5-g + 1P: Crown Panel Out-of-Plane Deformation

## Slide 52: 2.5-g + 1P: Frame of Crown Panel
Strains up to 2.5-g 165% DLL + 1P 150% DLL

## Slide 53: 2.5-g + 1P: Crown Panel Skin
Minimum principal strains up to 2.5-g 165% DLL + 1P 150% DLL

## Slide 54: 2.5-g + 1P: Crown Panel Minimum Gauge Skin
Back-to-back strains up to 2.5-g 165% DLL + 1P 150% DLL

## Slide 55: Design of Discrete Source Damage (DSD)
Crown panel diamond-shaped cut
Mid-bay to mid-bay including cutting the center frame
3 in. off mid-span centerline (CL)
51
Center Frame
Saw-Cut Contour
Dimensions in inches
Center Frame Web
Skin
Not to Scale

## Slide 56: Implemented DSD
View from the inside of the test article
Stringers
Center Frame

## Slide 57: FEM in the Vicinity of DSD
Element edge size at saw-cut tips ~0.05 in.
Saw-cut skin bay element edge size ~0.25 in.
Refined mesh connected to coarser mesh away from DSD using nodal values interpolation (RSPLINE functionality in MSC Nastran)
COLTS
Skin Top View
X
Y
HWB Center Section
Test Article
X
Z
Y

## Slide 58: Instrumentation
Results to be discussed based on
  Video image correlation in three dimensions (VIC-3D) full field displacement acquisition on the OML surfaces of crown and upper bulkhead panels
  Strain gauges (380 unidirectional and 36 rectangular rosettes, total 488 channels)

## Slide 59: Summary of DSD Analysis and Test Results
FEA executed up to 2.5-g DUL (150% DLL)
  Strain design values exceeded in skin sections of the crown panel
  Strain design values not exceeded in substructure (no catastrophic failure predicted)
Based on strain gauge and VIC-3D results
  First damage identified at 81.9% DLL at saw cut tip
  Several indications of damage progression identified between the initial and final failure
Final failure at 152.1% DLL

## Slide 60: 2.5-g DUL: Crown Panel Out-of-Plane Deformation

## Slide 61: 2.5-g DUL: Upper Bulkhead Out-of-Plane Deformation

## Slide 62: 2.5-g DUL: Upper Bulkhead Out-of-Plane Deformation
Pristine Crown
Crown with DSD

## Slide 63: Final Failure at 152% DLL (Crown)

## Slide 64: Final Failure at 152% DLL (Crown/Bulkhead)

## Slide 65: Conclusions – Pristine Test Article
HWB center section article testing completed successfully
  Technology Readiness Level (TRL) 5 for HWB fuselage structure demonstrated
Favorable comparison of test data and nonlinear analysis results
  Linear analysis relevant in rapid/preliminary sizing of substructure (stringers, frames)
  Nonlinear analysis needed for optimal structural performance under the design philosophy permitting early localized buckling and operating in significantly developed post-buckled regime

## Slide 66: Conclusions – Test Article with DSD
Successful completion of the HWB center section article testing in pristine and barely visible impact damage (BVID) conditions enabled final test to failure with DSD
  Failure load exceeded condition representative of transport category airframe certification standards with DSD (70% DLL)
FEA without damage progression capability rapidly developed and successfully applied to determine DSD geometry and guide test article instrumentation

## Slide 67: Conclusions – Damage Arresting Composites
Achieved the objective of 10% aircraft weight savings over state-of-the-art composites while maintaining safety margins and supporting advanced aircraft configurations
Manufacturability of complex build-up structures using PRSEUS concept demonstrated
Viability of the PRSEUS concept for non-conventional primary airframe structure demonstrated through combined load environment testing of the large test article representative of HWB center section (pristine, BVID, and DSD conditions)
Damage arresting capabilities of the PRSEUS concept verified experimentally in several building block tests under different load scenarios
  Need analysis capability to support the design and tailoring of damage arresting features
Ability to repair PRSEUS structures to restore the pristine load carrying capability also verified using existing repair techniques

## Slide 68
Questions?
nescacademy.nasa.gov

## Slide 69: Supplemental Material

## Slide 70: Long Beach, CA  Hampton, VA
MBB loaded on K-Loader at Boeing Long Beach
MBB loaded into Super Guppy at Boeing LB
MBB unloaded from Super Guppy at NASA LaRC
MBB unloaded from K-Loader at NASA LaRC

## Slide 71: Crown Panel Rework
Bonded patches (dry-to-dry) in blue
  Single stack thick (light blue)
  Double stack thick (dark blue)
Metallic fittings (magenta)
Metallic Fittings
Repair Patches
Single-Stack Thickness
Double-Stack Thickness